Yassine El karim1, Abdessamad Faik2, Yaroslav Grosu2 and Rachid Lbibb1

New metallic PCMs for thermal energy storage in concentrated solar power (CSP)

1 Laboratory of Sustainable Development, Faculty of Sciences and Technologies, Sultan Moulay Slimane University, 523 Beni Mellal, Morocco

2 CIC Energigune, Albert Einstein 48, 01510 Miñano (Álava), Espagne

Corresponding Author: yassineelkarim@gmail.com; Tel: (+212659087291)

Abstract- The aim of this paper is to investigate new classes of materials, metal alloys, as phase change materials (PCMs) for thermal energy storage (TES) application. In the first stage of this work, we discuss the considerations for the use of metal and metal alloys as PCMs for high temperature thermal storage applications, as well as summarize the literature on the limited research in this area. The second stage of this work consists to synthesis, analysis and characterize a set of binary metal alloys based on Mg, Al, Cu and Si.

# Keywords: Concentrated solar power (CSP), Thermal energy storage (TES), Phase change materials (PCM), Metal alloys, high temperature

# INTRODUCTION:

# Renewable energies are sources of clean, inexhaustible and more competitive energy. They differ from fossil fuels in their diversity, abundance and potential for use on the planet. Their costs are also falling, and the cost of fossil fuels is in the opposite direction of their present volatility. One of the drawbacks of renewable energies is the intermittency of its production, which have directly repercussions on the competitiveness against conventional energy sources. In order to overcome this limitation and increase its global efficiency, energy storage (ES) strategies are a key issue.

CSP is one of these key technologies for a renewable energy future and the IEA’s objectives are that CSP should be able to provide 11.3 % of the global energy needs by 2050 [1]. CSP has the inherent ability to store thermal energy, which makes this a key technology to achieve a                                            renewable energy future. There are three main types of thermal energy storage (TES) according

to the storage mechanism involved: sensible heat storage, latent heat storage and thermo-chemical storage [2]. Thermal energy storage in the latent heat of phase change materials (PCMs) has the advantage that a great amount of energy can be stored across a small temperature difference. PCMs for high temperature TES systems are actually based on molten salts or eutectic salts compounds [3]. However, the principal limitation of salts are their poor thermal conductivity, followed of other common limitation such as considerable thermal hysteresis, corrosion problems and high volume change during the melting [3.4.5]. In order to diminish these problems, pure metals and metal alloys have been proposed as possible candidates for TES, using their phase change enthalpy between solid and liquid state. The main components of these alloys are magnesium, aluminum, copper and silicon.

The first objective of this paper is to assess the use of metal and metal alloys for TES, as well as summarize the literature on the limited research in this area. The second aim of this work consists to synthesis, analysis and characterize a set of binary metal alloys based on Mg, Cu, Si and Al.

# State of the art on use of metal and metal alloys as TES materials MEDIA:

Thermal energy storage in the latent heat of phase change materials has the advantage that a great amount of energy can be stored across a small temperature difference. The higher the heat of fusion of a PCM, the more energy can be stored in it per unit mass. Therefore, a high heat of fusion is preferable. Other than the heat of fusion, there are a number of important properties that must be considered in PCM selection [5]: Melting temperature (Tm) ,low or no sub-cooling, thermal stability ,Chemical stability ,Cyclic stability ,Thermal conductivity ,Specific thermal capacity ,Low cost ,Availability ,Low toxicity and Compatibility with construction materials .

To compare the classes of the various PCMs that can be found in literature, a plot of the heat of fusion against the melting point of each candidate PCM is shown in Figure 1.

Fig. 1. Comparison of high temperature PCMs found in literature [5].

It is clear that the metallic PCMs and fluoride salts have melting temperatures that are very well suited for high efficiency power blocks.

Salts have a significant set of drawbacks that metallic PCMs generally do not exhibit:

- Salts are prone to subcooling, where metals generally have no or little subcooling.

- Salts have a large volume change over phase change.

- Salts have low thermal conductivity.

Thus, metallic phase change materials pose a set of significant advantages over that of salts.

Most likely, Birchenal and Telkes [6] were the first who have analyzed possibility to store the thermal energy by using the heat fusion of metals. Making a start from that work, Farkas and Birchenall [7] and Gasanaliev and Gama- taeva [8] report the thermal properties of some metallic alloys.

Table.I list the metal alloys with melting temperatures above 300°C proposed and studied by various researchers as high temperature PCMs. From the table, it appears that the A1-Cu, A1-Si, Al-Cu-Mg, Al-Mg-Zn and A1-Si-Mg eutectics have the best heat storage characteristics in the range to operate with fossil-fueled combustors. The Al-Si-Ni and Mg-Si eutectic has very good heat storage capacity at high temperature (over than 900°C), where it might find application in a solar power tower. Thus, eutectic compositions and pure substances are preferred as PCMs because of thermal stability and very small temperature range for phase change.

According to these conclusions, we were analyzed  different binary phase diagrams of the selected materials already proposed. Cu, Si and Mg metal alloys have being selected as potential latent heat storage (LHS) materials to be investigated by our group.

Table I. Several of current investigations about metal alloys for their use as potential HT-PCM in solar power generation technologies [6.7.8].

| Compound (mass %) | Melting point (° C) | Density | Enthalpy of melting |
| --- | --- | --- | --- |
| Al17Si53Ni30 | 1079 | 4290 | 962 |
| Si52Mg48 | 946 | 1900 | 757 |
| Al45Si40Fe15 | 869 | 3360 | 562 |
| Si49Mg30Ca21 | 865 | 2250 | 305 |
| Mg2Cu | 841 | - | 243 |
| Cu80Si20 | 803 | 6600 | 197 |
| Cu56Si27Mg17 | 770 | 4150 | 420 |
| Cu74Zn19Si7 | 765 | 7170 | 125 |
| Zn49Cu45Mg6 | 703 | 8670 | 176 |
| Al87.8Si12.2 | 580 | 2620 | 499 |
| Al46.3Cu49.1Si4.6 | 571 | 5560 | 406 |
| Al82Cu18 | 550 | 3170 | 318 |
| Mg13 Bi87 | 546 | 3090 | 181 |
| Al60.8Cu33.2Mg6 | 506 | 3050 | 365 |
| Mg60Cu25Zn15 | 452 | 2800 | 254 |
| Al60Mg34Zn6 | 450 | 2380 | 329 |
| Zn88.7Al11.3 | 382 | 6752 | 118 |
| Zn84Al8.7Mg7.3 | 344 | 6546 | 132 |
| Mg72Zn28 | 342 | 2850 | 155 |

# Method and experience:

The experimental process were  performed in CIC energiGUNE (Spain) .The binary metal alloys were produced by melting together  pure components in suitable proportion (Cu (Shots, 1-10 mm, 99.99%, Alfa S.A), Si (Lump,0.1-2.5 cm,99.99%, Alfa S.A ) , Al (Ingot, 99.98%, Alfa S.A) and Mg (Ingot, 99.98%, Alfa S.A).

The experiments run under a controlled argon flux. The systems were placed and closed inside of stainless steel reactor under argon atmosphere in order to avoid any possible oxidation of the alloys. Next, the reactor was introduced in a muffle electrical furnace at 750ºC for 2 hours. Before cooling, the molten alloy was mixed by a slight rotational movement in order to ensure a high homogeneity of the samples.

The Microstructural characteristics was examined by scanning electron microscopy (SEM) ,Quanta FEG 250, operated in high vacuum mode at 30 kV and with a back scattered electron detector (BSED).

The DSC measurements were performed using STA 449 F3 Jupiter with a heating rate of 10 °C/min under a constant stream of argon with a flow rate of 50 ml/min.

The density  of the materials investigated was determined by helium pycnometer AccuPyc II 1340 from metrics coupled to a digital scale (Mettler Toledo).

# Results and DISCUSSION:

Fig. 2. Metal alloys with different compositions

To conduct the characterization of the alloys, the samples (Fig.2 ) were mechanized by different techniques as shown in fig.3 . In this way, the turning and grinding mechanizing processes were carried out in CIC energiGUNE by a diamond saw and a disc grinder respectively.

Fig. 3. Samples mechanized by different techniques

Fig.4 provides a strong experimental confirmation of the existence of only two phases after the solidification processes. In general, the observed structures by SEM confirm the eutectic nature of the investigated alloys

Fig. 4. SEM images (BSED) of Mg-Cu eutectic at 5000-x magnification

In Fig.5 only one endothermic peak is observed in the solid– liquid transition, this peak corresponds to the melting of the eutectic mixture in agreement with the phase diagram.

Fig.5.Melting and solidification temperatures and enthalpies obtained from DSC results at 10 °C/min heating/cooling rates.

Table.II shows current investigations, where, metals are proposed as HT-PCMs for solar power applications, as those of most important binary metal alloys and inorganic salts from literature

Table II. Comparison of thermophysical properties of eutectic alloys investigated in this work with some other metal alloys and molten salts.

| Compound |  | Melting point (° C) | Density | Heat capacity | Enthalpy of melting |  | Thermal conductivity | Volumetric heat storage | reference |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Binary Alloys (Cu, Si ,Al and Mg) | From To | 488 702 | 2459 6500 | 788 665 | 232 144 | 104 96 |  | 561 1050 | PW |
| Mg72Zn22 |  | 342 | 2850 | 711 | 155 | 67 |  | 441 | [9] |
| Mg13Bi87 |  | 546 | 3090 | 530 | 181 | 53 |  | 559 | [10] |
| PbCl2 |  | 501 | 5600 | NA | 78 | 0.69 |  | 436 | [11] |
| NaCl/MgCl2 |  | 450 | 2240 | 960 | 429 | 0.93 |  | 960 | [6] |
| NaCl/CaCl2/MgCl2 |  | 424 | 2500 | 1190 | 190 | 0.83 |  | 475 | [12] |
| MgCl2-SrCl2 |  | 500 | 2100 | 670 | 281 | 1.08 |  | 590 | [13] |

PW stands for present work

NA not available

By the comparison of metal alloys properties and salts properties listed in Table.II, it can be seen that the main advantages of these metal alloys compared with inorganic salts are their high thermal conductivities, which are two and even three orders of magnitude higher. On the other hand, heats of fusion of investigated alloys are lower than those values in some salts.

# Conclusion:

The obtained results show the potentiality of these metal eutectic alloys, based on Cu, AL, Mg and Si, as storage media in the development of a new concept of thermal energy storage systems. It has been shown that the high thermal conductivity of metal alloys represent one of the main advantages of their use as PCMs due to its possibility to reduce the heat exchanger area, which has a direct influence on the final cost of the heat exchanger.

- Acknowledgements

The author would like to thank TES groups in CIC Energigune for their help and support.

- References

- International Energy Agency 2010.Technology Roadmap [Report] / IEA. - Paris : IEA

- L.F. Cabeza, E. Galindo, C. Prieto, C. Barreneche, A. Inés Fernández, Key performance indicators in thermal energy storage: survey and assessment, Renew. Energy 83 (2015) 820–827..

- M. Liu, W. Saman, F. Bruno, Review on storage materials and thermal performance enhancement techniques for high temperature phase change thermal storage systems, Renew. Sustain. Energy Rev. 16 (2012) 2118–2132.

- A. Gil, M. Medrano, I. Martorell, A. Lázaro, P. Dolado, B. Zalba, L.F. Cabeza, State of the art on high temperature thermal energy storage for power generation. Part 1 –Concepts, materials and modellization, Renew. Sustain. Energy Rev. 141 (2010)31–55.

- M.M. Kenisarin, High-temperature phase change materials for thermal energy storage, Renew. Sustain. Energy Rev. 14 (2010) 955–970.

- [4] C.E. Birchenall, A.F. Riechman “Heat Storage in Eutectic Alloys” Metallurgical Transactions A-physical Metallurgy and Materials Science, 11(8) (1980) 1415-1420.

- D.Farkas and C.E. Birchenall, “New Eutectic Alloys and Their Heats of Transformation”. Metallurgical transformation A, 16A (1985) 323–328.

- A. M. Gasanaliev and B Yu Gamataeva, “Heat-accumulating properties of Melts”. Russian Chemical Reviews. 69 (2000) 179 – 186.

- P. Blanco-Rodríguez, J. Rodríguez-Aseguinolaza, E. Risueño, A. Faik, M. Tello, S. Doppiu Corrigendum to “Thermophysical characterization of Mg-51%Zn eutectic metal alloy: A phase change material for thermal energy storage in direct steam generation applications”, Energy 75 (2014) 630.

- D. Fang, Z. Sun, Y. Li, X. Cheng  "Preparation, microstructure and thermal properties of Mg—Bi alloys as phase change materials for thermal energy storage",Applied Thermal Engineering 92 (2016) 187–193

- X. Wei, M.Song, W. Wang, J. Ding and J. Yang, “Design and thermal properties of a novel ternary chloride eutectics for high-temperature solar energy storage”. Applied Energy, 156 (2015) 306–310.

- Trunin AS.Designing and investigations of salt systems for solar energy utilization. Utilization of sun and other radiation sources in materials research.Kiev:NaukovaDumka;1983.p.228–38.

- Maru HC, Dullea JF, Kardas A, Paul L, Marianowski LG, Ong E, et al. Molten salts energy storage systems. Chicago, IL: Final Report of the Institute of Gas Technology; 1978